XIAMEN DITAI IMP.& EXP. CO.,LTD

8FL, Hongsheng Building, West Hexiang Road, Xiamen, Fujian, China

TEL:+86-18859285106 FAX:86-592-2680880 E-mail:amy.zhang@xmditai.com

Factory Supply High Purity Aluminium Stearate Powder with Competitive Price

1. Product introduction:

Aluminium Stearate
CAS Number: 637-12-7 
Molecular formula: C54H105AlO6 
Molecular weight: 877.40


3. Product specification:

| Assay item | Unit | Standard Index |
| --- | --- | --- |
| Appearance | / | White Powder |
| Aluminium Content | % | 4.0-5.2 |
| Free Acid | % | ≤6.0 |
| Heating loss | % | ≤1.50 |
| Melting Point | 0C | 155-170 |
| Fineness(200 mesh) | % | ≥99.0 |

4. Application:

a.It can be used as raw material for the manufacture of metal rust inhibitor.

b.It can be used as a waterproofing agent for building materials, a brightening and thickening agent for coatings and inks. 

c.It is used as an emulsifier for cosmetics and a lubricant for plastics, etc. 

d.It can also be used as a heat stabilizer for polyvinyl chloride.
​

Package: 25Kg per paper bag, with inner PE bag. 
Storage: In cool and draught place, no exposure to moisture, heat, fire or corrosion, not pile with acid, Bases and corrosion goods.

​

XIAMEN DITAI CHEMICALS CO., LTD
8FL,Hongsheng Building,West Hexiang Road,Xiamen, China

ISO9001:2015  Certificated